Cleanroom Class 100 Nitrile Gloves 百级净化间丁晴手套 (CN-100D)

Features:

- Manufactured from high quality Acrylonitrile-Butadiene Rubber (NBR) synthetic co-polymer

- Resistance wide range of solvent chemicals

- Excellent sensitivity, superior strength and flexibility

- Accelerator free, sulfur free, Itching Free

特点:

- 由高品质的丁腈橡胶（NBR）合成共聚物制成

- 耐多种化学品溶剂

- 优越的灵敏度，高强度，高弹性

- 不使用添加剂，无硫化过程，不致痒

Process :

- Laundered with 0.2 micron filters using 18.2 Mohm EDI water system

- Inspection and packed in Clean-room Class 100/ ISO 5

过程:

- 使用高纯净水(18.2 Mohm, 0.2um过滤膜)系统洗涤

- 在百级净化间检查，包装

Applications:

- Critical Cleanroom Environment, Semiconductor Industries, Flat Panel Displays

应用:

- 广泛的应用于净化环境, 半导体行业, 平面显示器等行业

Product Information 产品信息:

- Cleanliness 洁净度

| TEST ITEM | SPECIFICATION |
| --- | --- |
| Particle Counts(Orbital shaker, 0.5um & larger) | <1000 counts/cm2 |
| Traceable Ions | Fluoride (F) | N/A |
|  | Chloride (Cl) | <0.1mg/g |
|  | Nitrite (NO2) | N/A |
|  | Bromide (Br) | N/A |
|  | Nitrate (NO3) | <0.2mg/g |
|  | Phosphate (PO4) | N/A |
|  | Sulfate (SO4) | <0.02mg/g |
|  | Total Anion | <0.35mg/g |
| Non-Volatile Residue IPA/Hexane | <20mg/g |
| FT-IR (Test for major organic contaminants) | No Silicone oil, No Amide & No DOP |

(Tested in accordance to Seagate Method—Doc.Number:35344-001 Rev.P)

2. Dimensions 尺寸(Ref Doc: ASTM D3578/D6319)

| Glove Size 12” 12”手套尺寸 | Palm Width 手掌宽 (mm) | Length 长度 (mm) | Thickness 厚度(mm) |
| --- | --- | --- | --- |
| Small 小码 (S) | 85 + 5 | min 290 | > 0.06 |
| Medium 中码 (M) | 95 + 5 | min 290 | > 0.06 |
| Large 大码 (L) | 105 + 5 | min 290 | > 0.06 |

3. Physical Properties 物理性质(Ref Doc: ASTM D6319/D412)

| Strength Elongation强度/伸长率 | Before Aging老化前 | After Aging老化后 |
| --- | --- | --- |
| Tensile Strength拉伸强度 (MPa) | Min 14 | min 14 |
| Ultimate Elongation 断裂伸长率(%) | Min 500 | min 400 |

4. ESD Properties防静电性质(Ref Seagate Doc: ST1248 Rev. C)

| Surface Resistivity表面电阻 (ohms/square) | Maximum 1010 |
| --- | --- |
| Static Decay衰减时间(sec) | Maximum 2 |
| Triboelectric charge摩擦电压 (volts) | Maximum 20 |

5. SEM/EDX Test表面电镜测试 (Ref Seagate Doc: 35366-001 Rev. H)

| Item项目 | SPECIFICATION规格 |
| --- | --- |
| MgSiO (counts/cm2) | <50 |

6. Copper Strip Test铜腐蚀性   :	No Discoloration无变色

7. Quality Assurance品质保证  :	Manufactured under ISO9001:2008 Quality System and ISO14001:2004 Environment System/公司通过 ISO9001:2008 及ISO14001:2004体系

8. Packaging		包装方式       :	100 pieces of gloves per double poly-bags

10 bags per carton  100只每包，双袋包装，10包每箱

# Text boxes

www.cleanera.net

Product Specification

Product Specification

www.cleanera.net